## Slide 1: Wide-Range 3D Magnetic Field Sensing in a 90°-Bent Geometry Enabled by Spin-Orbit Torque P. K. Mishra, H. Rahaman, R. Maddu, B. Jamshed, S. Das, and S.N. Piramanayagam
Division of Physics and Applied Physics
Nanyang Technological University, Singapore

## Slide 2: Introduction to Magnetic Sensors
Magnetic sensor: electronic device to detect the magnetic flux

## Slide 3: SOT Driven-DW Based Sensors
Authors | Stack | Characteristics | Dynamic range
Li et al. (2021) | Si/SiO2/Ta/CoFeB/MgO/Ta | SOT/DW motion | ±10 Oe, ±10 Oe, ±4 Oe
Guo et al. (2022) | Si/SiO2/W/CoFeB/MgO/Ta | SOT/domain nucleation | ±20 Oe, ±20 Oe, ±20 Oe
Su et al. (2023) | Si/SiO2/Ta/Pt/Co/Ta | SOT/DW motion | ±30 Oe, ±25 Oe, ±10 Oe
Tao et al. (2024) | MgO (0 0 1)/L10 FePt | SOT/domain nucleation | ±200 Oe, ±200 Oe, ±200 Oe
[1] Li et al., Nat Electron 4, 179–184 (2021).
[2] Guo et al., Appl. Phys. Lett. 120, 232404 (2022).
[3] Su et al., Adv. Funct. Mater. 33, 2211752 (2023).
[4] Tao et al., ACS Appl. Mater. Interfaces 16, 27917-27925 (2024).

## Slide 4: Circuit Diagram of Sensor
normally close
normally open
Terminals 3 & 4 are connected to the current source
Terminals 2 & 1 are connected to a nanovoltmeter
Li et al., Nat Electron 4, 179–184 (2021).
Mechanical rotation
I <->V terminal interchange

## Slide 5: Schematic of Proposed Device and Working Mechanism
I
A
B
C
D
Measure:-
HX field Horizontal Hall bar AB terminals
Hy field Vertical Hall bar CD terminals

## Slide 6: In-plane field sensing
t = 0.8 nm
time
J
Hz,sat
H
Hip
time
J = 1.63×1011 A/m2
PW = 0.1 s
-350 Oe
-140 Oe
140 Oe
350 Oe
-350 Oe
-140 Oe
140 Oe
350 Oe
Spin-up
Spin-down
Large in-plane dynamic range
Angular field sensing

## Slide 7: Out-of-plane field sensing
Highest-ever reported dynamic range in SOT-based sensor
Excellent repeatability  Good durability